## Slide 1: Blech Effect in Interconnects: Applications and Design Guidelines
Ali Abbasinasab
Malgorzata Marek-Sadowska

## Slide 2: Overview
Introduction
Material Migration: Multiphysics
  Blech Effect
CAD Model: New Mortality Criterion
Conclusions

## Slide 3: Trends in Interconnect Design Introduction
Current Status
ITRS 2014-2020 (Reliability Challenge)
TCAD / Multiphysics Simulations
Devices, Interconnects and Packaging (nanoscale process)
  Chemical, thermal, mechanical and electrical properties of new materials: capping (MnSiO, CuAl , CuTi….), liners (Co, Ru) and thickness, air-gap, low-k ILD
  Technology, dual-damascene
CAD
  Accurate Compact Models
  Chip level assessment
Chart: Number of metal levels
| 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024 | 2025 | 2026
Number of metal levels (includes ground planes and passive devices) | 11 | 12 | 12 | 12 | 12 | 12 | 13 | 13 | 13 | 13 | 14 | 14 | 14 | 14 | 15 | 15 | 15 | 15 | 16 | 16
Chart: Total wire length (m/cm2) (6 levels)
| 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024 | 2025 | 2026
Total interconnect length (m/cm2) – Metal 1 and five intermediate levels, active wiring only [1] | 1852 | 2222 | 2632 | 3125 | 3704 | 4167 | 4762 | 5291 | 5917 | 6667 | 7463 | 8403 | 9434 | 10526 | 11905 | 13333 | 14948 | 16779
Chart: Jmax (MA/cm2) – int wire ( 105C)
| 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024 | 2025 | 2026
Jmax (MA/cm2) – intermediate wire (at 105ºC) [7] | 1.16 | 1.32 | 1.5 | 1.68 | 1.79 | 1.81 | 2.01 | 2.29 | 2.34 | 2.59 | 2.88 | 2.94 | 3.26 | 3.76 | 4.23 | 4.5

## Slide 4: Material Migration Introduction
Material-migration
Material transportation caused by the gradual movement of the atoms in conductor
  Electromigration
  Stressmigration
  Thermomigration
Criticality: Technologies and Applications
  Process, Manufacturing, 3D Integration, Packaging
  Power and Signal/Clock Lines
  Long-Term/Constantly-In-Use Chips: Automotive, Servers and Routers

## Slide 5: Material Migration: Multiphysics
Material concentration change (vacancy transport) described by continuity equation:
Electro-migration :
Thermo-migration :
Stress-migration :
Diffusion-migration :
Notes: FLUX
Change in atom concentration (or vacancy concentration) can be caused by different sources ranging from electrical, mechanical and thermal to the material chemical properties.
Material concentration change or vacancy transport can be described by continuity equation:
where Cv is the vacancy concentration, J is the vacancy flux and G is the source/sink model for generation and annihilation of vacancies.
Electro-migration
  Electron wind:
Stress-migration
    Back stress:
Thermo-migration
    Joule Heating:
4th A local variation in the atomic concentration can then occur during the fabrication and mostly in the grain boundary regions during the crystal growth. It can have an important impact on the degradation caused by particles diffusion induced migration.
In the continuity equation, G can be representing both vacancy generation and vacancy annihilation. When the concentration of vacancy is larger than its equilibrium value, vacancies are produced, while vacancies are annihilated when their concentration is less than the equilibrium value.
Tau is the lifetime of a vacancy in the presence of sinks (surface, dislocation) – not necessarily a constant.
These equations are pretty complicated – difficult to use by a designer.
FLUX
Change in atom concentration (or vacancy concentration) can be caused by different sources ranging from electrical, mechanical and thermal to the material chemical properties.
Material concentration change or vacancy transport can be described by continuity equation:
〖𝜕𝐶〗_𝑣/𝜕𝑡+𝛻. 𝐽=G
where Cv is the vacancy concentration, J is the vacancy flux and G is the source/sink model for generation and annihilation of vacancies.
Electro-migration
  Electron wind: 𝐽_𝑒𝑚=−(𝐷𝐶_𝑣)/𝑘𝑇 𝑒𝑍^∗ 𝑗𝜌
Stress-migration
    Back stress: 𝐽_𝑠𝑚= −(𝐷𝐶_𝑣)/𝑘𝑇 𝑓Ω𝛻σ
Thermo-migration
    Joule Heating: 𝐽_𝑡𝑚= −(𝐷𝐶_𝑣)/𝑘𝑇 𝑄^∗/𝑇 𝛻T
4th A local variation in the atomic concentration can then occur during the fabrication and mostly in the grain boundary regions during the crystal growth. It can can have an important impact on the degradation caused by particles diffusion induced migration.
Minor improvement, in the interests of time, we will discuss it later.
By adding all different fluxes the total mass flux is
In the continuity equation, G can be represented both vacancy generation and vacancy annihilation. When the concentration of vacancy is larger than its equilibrium value, vacancies are produced, while vacancies are annihilated when their concentration is less than the equilibrium value. Therefore, G is modeled as:
While tau is considered to be a constant number which we noticed that it’s not true depending on crystalline oriantationa nd grain size, in our simulation we improved it by modeling as pi r 2 which represent the the average time that a vacancy travels in order to have a relaxed lattice which is proportional to grain size, radius. Tau basically is the lifetime of a vacancy in the presence of sinks (surface, dislocation)
Electro-migration
  Electron wind: 𝐽_𝑒𝑚=−(𝐷𝐶_𝑣)/𝑘𝑇 𝑒𝑍^∗ 𝑗𝜌
Stress-migration
    Back stress: 𝐽_𝑠𝑚= −(𝐷𝐶_𝑣)/𝑘𝑇 𝑓Ω𝛻σ
Thermo-migration
    Joule Heating: 𝐽_𝑡𝑚= −(𝐷𝐶_𝑣)/𝑘𝑇 𝑄^∗/𝑇 𝛻T

## Slide 6: CAD models
What matters to a Designer or a CAD Engineer?
Geometry and Topology
  L, W, T and Interconnects Configuration
Electrical
  Conductivity and Current Density ()
Thermal
  Joule Heating (Thermal Expansion Coefficient)
Chemical/Physical
  Material (Activation energy, Young’s modulus, Diffusion…)

## Slide 7: Blech Effect Material Migration: Multiphysics
Competition between two main forces
In steady state, back-stress force balances electron wind force
If stress required for void nucleation is not reached at cathode end in steady state, no void will nucleate
Critical Tensile Stress
Hydrostatic Stress Distribution
cathode
anode
Notes: P2P where Ps are vias
jL provides a mortality filter – compared to a value characteristic for specific technology.
Effects of these four different driving forces which contribute to the EM process are not equal. Their typical contributions in terms of atomic flux are
Blech studied EM in
Electron Wind Force:
Back Stress Force:
simple end-to-end interconnects and observed that there is no mass transport when current density is less than a certain threshold value for a given wire length
It is suggested that the presence of a back flow of atoms due to the back stress at the anode end opposes the electron wind. If the stress difference between the cathode and anode ends is less than that needed for void nucleation, the stress profile will evolve towards a steady state at which point the net atomic flux becomes zero and the wire is considered immortal. The condition of and being equal is mathematically expressed as
Electromigration is electron-flow induced diffusion of atoms in a metal line.
Z* - effective atomic charge number, is electrical resistivity of metal, is stress.
P2P where Ps are vias how JL does not work for multiple Ps
Provides an mortality filter in terms of some critical product for immortality check
Effects of these four different driving forces which contribute to the EM process are not equal. Their typical contributions in terms of atomic flux are |𝐽_𝑡𝑚 |≪|𝐽_𝑚𝑚 |< |𝐽_𝑠𝑚 | ≈|𝐽_𝑒𝑚 |
Blech studied EM in
Electron Wind Force:
𝑭_𝒆𝒎=𝒆𝒁^∗ 𝑬= 𝒆𝒁^∗ 𝒋𝝆= −𝒆𝒁^∗ 𝑽 →┴( ) 𝑱_𝒆𝒎=−(𝑫𝑪_𝒗)/𝒌𝑻 𝒆𝒁^∗ 𝒋𝝆
Back Stress Force:
𝑭_𝒔𝒎= 𝒇Ω𝛁𝛔 →┴( ) 𝑱_𝒔𝒎= −(𝑫𝑪_𝒗)/𝒌𝑻 𝒇Ω𝛁𝛔
simple end-to-end interconnects and observed that there is no mass transport when current density is less than a certain threshold value for a given wire length
He suggested that the presence of a back flow of atoms due to the back stress at the anode end opposes the electron wind. If the stress difference between the cathode and anode ends is less than that needed for void nucleation, the stress profile will evolve towards a steady state at which point the net atomic flux becomes zero and the wire is considered immortal. The condition of 𝐽_𝑠𝑚 and 𝐽_𝑒𝑚 being equal is mathematically expressed as
Electromigration is electron-flow induced diffusion of atoms in a metal line.

## Slide 8: Blech Effect Material Migration: Multiphysics
    jLBlech is valid for a simple single bounded wire
JL
(0.5J)L
J(0.5L)
Current density
Hydrostatic Stress JL
Critical Stress
Critical Stress
Critical Stress

## Slide 9: Motivation and Problem Description CAD Model: new Mortality Criterion
jL is solely used in industry-standard P/G and signal integrity solutions and tools.
  Existing EM analysis solutions are not accurate for complex wire structures
  Thus they need designers’ time-consuming manual adjustments
QUESTION: Are j and L the only information needed for capturing EM failure precisely?
  We reveal the weakness of jL-based methods by motivating examples
  j and L are weaker predictors for more complicated interconnect structures
  j and L don’t include atomic flux, geometry and material properties correctly

## Slide 10: Past Works CAD Model: new Mortality Criterion
Other advanced models:
  [Riege TED‘98]:
  Find the longest anode-cathode path with respect to jL
    Does not capture interconnect interaction accurately.
    Not applicable to complex structures
  Via Vector [Park RPS’10]:
  Calculate the atomic flux divergence at via nodes
    Does not offer a compact model or a systematic analysis
    Lack of explanation for experimental observations
Notes: People observed while sigma JL is true yet the hydrostatic distribution is different

## Slide 11: Motivation and Problem Description CAD Model: new Mortality Criterion
    Same longest anode-cathode path, yet different hydrostatic stress distribution
Notes: Adding a limb to a point-to-point structure
The effective product () is calculated and compared to the . In this method, is assumed to be equal to where is the critical tensile stress for a void to nucleate. This assumption can be valid for symmetric structures. However, in multi-branch nets with arbitrary topology, may reach but void nucleation may not occur because the stress at the cathode may be less than. Such situations occur for critical compressive stress for low-k dielectric breakage or extrusion
The effective 𝑗𝐿 product (𝑗𝐿_𝑒𝑓𝑓) is then calculated and compared to the 𝑗𝐿_(𝑐𝑟𝑖𝑡_𝑛𝑢𝑐). Using their method the failure due to the void saturation can be checked by comparing 𝑗𝐿_𝑒𝑓𝑓 to 𝑗𝐿_(𝑐𝑟𝑖𝑡_𝑠𝑎𝑡). In this method, Δ𝜎_𝑚𝑎𝑥 was assumed to be equal to 2𝜎_(𝑐𝑟𝑖𝑡_𝑛𝑢𝑐) where 𝜎_(𝑐𝑟𝑖𝑡_𝑛𝑢𝑐) is the critical tensile stress for a void to nucleate. This assumption can be valid for symmetric structures. However, in multi-branch nets with arbitrary topology, 𝑗𝐿_𝑒𝑓𝑓 may reach Δ𝜎_𝑚𝑎𝑥 but void nucleation may not occur because the stress at the cathode may be less than〖 𝜎〗_(𝑐𝑟𝑖𝑡_𝑛𝑢𝑐). Such situations occur for critical compressive stress for low-k dielectric breakage or extrusion

## Slide 12: Motivation and Problem Description CAD Model: new Mortality Criterion
jLBlech can be used only for single bounded wire (due to adjacent wire segment interaction)
Current density
Hydrostatic Stress JL
JL
JL
JL
JL
Notes: In all cases jl is the same value yet hydrostatic stress is different
Max value is different
Convetional simulation results show that p2p Jl is not applicable directly to complex structures
Sigma jl is not a correct criterion

## Slide 13: Motivation and Problem Description CAD Model: new Mortality Criterion
What is missing in previous models?
Electrical
  Atomic flux divergence
Geometry (studied only for single bounded wire & other extensions are inaccurate)
  Length, Width, Thickness Effect
  Angle Effect: Current crowding
  Via cut surface, thickness and perpendicularity
Layout Topology
  Multi-branch structure and remote connections
  Passive segments: dummy vias and reservoirs
Damascene Materials
  Interface Thickness: Barrier and Capping
  Grain boundaries configuration
  Interface Properties: Stiffness (Young’s Modulus)
Can be compacted into a diffusion coefficient
Notes: Electrical, geometrical properties are not captured properly

## Slide 14: New Compact Model CAD Model: new Mortality Criterion
Notes: The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual and the actual stress distribution based on the atom conservation principle:
where is the concentration of atoms along the net and is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of depends linearly on the concentration of atomic lattice sites
RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual (𝑗𝐿)_𝑒𝑓𝑓 and the actual stress distribution based on the atom conservation principle:
where 𝑐 is the concentration of atoms along the net and 𝑁_0 is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of 𝜎 depends linearly on the concentration of atomic lattice sites 𝐶 by

## Slide 15: New Compact Model CAD Model: new Mortality Criterion
Atom Accumulation = Atom Depletion
Notes: RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual and the actual stress distribution based on the atom conservation principle:
where is the concentration of atoms along the net and is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of depends linearly on the concentration of atomic lattice sites
RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual (𝑗𝐿)_𝑒𝑓𝑓 and the actual stress distribution based on the atom conservation principle:
where 𝑐 is the concentration of atoms along the net and 𝑁_0 is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of 𝜎 depends linearly on the concentration of atomic lattice sites 𝐶 by

## Slide 16: New Compact Model CAD Model: new Mortality Criterion
Atom Accumulation = Atom Depletion
Notes: RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual and the actual stress distribution based on the atom conservation principle:
where is the concentration of atoms along the net and is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of depends linearly on the concentration of atomic lattice sites
RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual (𝑗𝐿)_𝑒𝑓𝑓 and the actual stress distribution based on the atom conservation principle:
where 𝑐 is the concentration of atoms along the net and 𝑁_0 is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of 𝜎 depends linearly on the concentration of atomic lattice sites 𝐶 by

## Slide 17: New Compact Model: HOWTO CAD Model: new Mortality Criterion
Notes: RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual and the actual stress distribution based on the atom conservation principle:
where is the concentration of atoms along the net and is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of depends linearly on the concentration of atomic lattice sites by
RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual (𝑗𝐿)_𝑒𝑓𝑓 and the actual stress distribution based on the atom conservation principle:
where 𝑐 is the concentration of atoms along the net and 𝑁_0 is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of 𝜎 depends linearly on the concentration of atomic lattice sites 𝐶 by

## Slide 18: New Compact Model CAD Model: new Mortality Criterion
    Simple Net
Notes: RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual and the actual stress distribution based on the atom conservation principle:
where is the concentration of atoms along the net and is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of depends linearly on the concentration of atomic lattice sites by
RED BLUE &&& area && deltaC
How to use: JL belch itself + new!!!
Volume! Rectangular!
The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression.
This model offers a systematic way of determining the actual (𝑗𝐿)_𝑒𝑓𝑓 and the actual stress distribution based on the atom conservation principle:
where 𝑐 is the concentration of atoms along the net and 𝑁_0 is the total number of atoms. The total number of atoms must be equal in the initial state and in the steady state. In other words, the number of atoms accumulated and depleted in different segments of the net is zero:
From Blech’s equation (2), the stress within a segment
A first order approximation of 𝜎 depends linearly on the concentration of atomic lattice sites 𝐶 by

## Slide 19: New Compact Model Improved Blech Effect
    Complex Net
Notes: Interesting results illustrate how layering can affect EM performance. (limbs)
The topology is the same yet the part of net which conservation holds true is different, due to the blocking via that was enabled through dual damascene
A multi-segment net. is the same either segment a1a2 is connected to b1 as a side branch directly in the same layer or a1’a2’ to b1’ with a via through the lower layer. Red and green dots indicate via above and via below, respectively. Blue is the site of a potential via. Hydrostatic stress along the broken line near the interface is shown at the bottom (j).
A multi-segment net. 𝒋𝑳_𝒆𝒇𝒇=𝒎𝒂𝒙𝚺𝒋𝑳 is the same either segment b'd' is connected to b' as a side branch directly in the same layer or with a via through the lower layer. Red and green dots indicate via above and via below, respectively. Hydrostatic stress along the broken line near the interface is shown at the bottom (j=𝟏𝟎𝒎𝑨/〖𝒖𝒎〗^𝟐).

## Slide 20: New Compact Model CAD Model: new Mortality Criterion
Simulation Parameters T=459K, J=40MA/cm2 , Critical Stress =120MPa
    Current Flows in Different Directions Also Impact Each Other
Critical Stress
Notes: Interesting results
In addition to current density, the stress growth in an interconnect t depends not only on its geometry but also on the geometry of other segments of the same net. The effect of geometry, including length, width and thickness are all captured by and
This figure shows the effect of length of adjacent segments. In both nets, all segments carry the same current density j, flowing into the middle via. This can also be explained by the back stress built up in a shorter segment. In net II, the shorter segment sucks fewer atoms from the middle via compared to symmetric situation in net I.
Interesting results
In addition to current density, the stress growth in an interconnect t depends not only on its geometry but also on the geometry of other segments of the same net. The effect of geometry, including length, width and thickness are all captured by (𝑗𝐿)_𝑒𝑓𝑓=max┬█(𝑎𝑙𝑙 𝑗𝑢𝑛𝑐𝑡𝑖𝑜𝑛 @𝑝𝑎𝑖𝑟𝑠 𝑖,𝑗)⁡∑1_𝑘▒〖𝑗_𝑘 𝐿_𝑘 〗 and ∑1_(𝑠𝑒𝑔𝑚𝑒𝑛𝑡𝑠 𝑘)▒(𝜎_(𝑘−𝑎𝑛𝑜𝑑𝑒)+𝜎_(𝑘−𝑐𝑎𝑡ℎ𝑜𝑑𝑒))/(2𝐵_𝑘 ) 𝑉_𝑘=0
This figure shows the effect of length of adjacent segments. In both nets, all segments carry the same current density j, flowing into the middle via. This can also be explained by the back stress built up in a shorter segment. In net II, the shorter segment sucks fewer atoms from the middle via compared to symmetric situation in net I.

## Slide 21: New Compact Model CAD Model: new Mortality Criterion
    Segments with No Current Also Impact Active Segments
Critical Stress
better
worse
Notes: Extension matters, adding extension in anode is detrimental while at cathode is helpful!
The effects of passive elements (i.e. metal extensions with zero current) such as those added at cathode (reservoir), or anode (sink), or dummy vias have been investigated in many works [17]. However, a compact model suitable for CAD tools that can explain and model the underlying physics has not been proposed before.

## Slide 22: New Compact Model (passive elements) CAD Model: new Mortality Criterion
The critical current density for interconnect void nucleation in a wire connected to a passive reservoir and a sink is
    Proposed Compact Model Holds True For Passive Elements
Notes: Our method not only explains the active segments but also offers a general model for reservoir and sink extension
This figure shows an interconnect of a length L. This segment is connected to a reservoir and sink of lengths and respectively. Solving our model for this net is as shown in this slide.
Our method not only explains the active segments but also offers a general model for reservoir and sink extension
Fig 5 shows an interconnect of a length L. This segment is connected to a reservoir and sink of lengths 𝐿_𝑟 and 𝐿_𝑠 respectively. Solving equations (2) and (14) for the net shown in Fig 5 is as follows:
The critical current density for extrusion can be similarly obtained.

## Slide 23: Material Effects on Lifetime CAD Model: new Mortality Criterion
    Steady state analysis does not capture temporal effects of microstructure and material properties
low diffusivity
region
Bm
B1~140Gpa
B1~140Gpa
Notes:   The bulk modulus ( or ) of a substance measures the substance's resistance to uniform compression. It is defined as the ratio of the infinitesimal pressure increase to the resulting relative decrease of the volume.
  We think that it can be explained by B,
  Slows down the diffusion path at interface
  The wire live safely under the critical stress for a long time and reach to SS in a much longer time.
  This also can be used for EM performance improvement
  B=-V dp/dv

## Slide 24: Applications Explored New Mortality Criterion
  EM-resilient Design Guideline:
    Partial widening
      Decreasing width –if helps!
    Round L shape connection(avoid current crowding)
    Passive Extention
    EM-tolerant configuration
    Routing through alternative paths and layers!
    Multiple vias, Dummy Vias

## Slide 25: Conclusions
DONEs:
  New compact model that captures
    Physical and Electrical Impact
    Explains wire segments interactions
TODOs:
  EM-Resilient Design Guidelines
    Can be readily developed based on the proposed model